## Slide 1
Huiqiu Yuan
Department of Physics, Zhejiang University, CHINA
Field-induced Fermi surface reconstruction near the magnetic quantum critical point in CeRhIn5
Workshop on Heavy Fermion Physics: Perspective and Outlook, IOP, CAS, 2012/1/7-9

## Slide 2: Collaborators
Zhejiang U:
Lin Jiao
Tian Shang
Ye Chen
Jinglei Zhang
LANL:
Yoshimitsu Kohama
Marcelo Jaime
John Singleton
Eric Bauer
H. O. Lee
Joe Thompson
MPI-CPfS:
Frank Steglich
Ramzy Daou
Sungkyunkwa U:
Tuson Park
Rice U:
Qimiao Si

## Slide 3: OUTLINE
Introduction
The H-T phase diagram of CeRhIn5
Field induced changes of Fermi surface
Summary and outlook

## Slide 4
The global phase diagram in Kondo Lattice
H=Hf+Hc+Hk
= + +
G=Innn/Inn:
spin frustration
AFs: AFM with small FS, No static Kondo screening
PML: HF Fermi liquid
Kondo screening fully developed
AFL: Intermediate region.
Kondo screening develops
inside AFM state
Lifshitz transition
QM Si, Phys. B (2006)
I: Local QCP
II: SDW-type QCP
Notes: Our results seem to be able to be described by the global phase diagram in Kondo lattice proposed by Qimiao Si. Here the parameter G describe the degrees of spin frustrations, that is the ratio of the antiferromagnetic next-nearest-neighbor interaction over the nearest neighbor one and jK is antiferromagnetic Kondo intereaction. From this phase diagram, one can see that there exists two type of Quantum critical points: the first one is the local quantum criticality, which shows a direct change from AFM with small fermi surface to a paramagnet with large Fermi surface. In this case, the f-electron is delocalized while crossing the QCP. The second scenario is the SDW-type quantum criticality. In this case, the Kondo screening develops inside the AFM state, leading to an increase of Fermi surface volume even inside the AFM state. With further increasing the Kondo coupling Jk, the AFM state is suppressed and converted to a paramagnetic state. The SDW scenario seems to nicely describe our experimental findings in CeRhIn5.

## Slide 5
YbRh2Si2: Prototype of local QCP
YbRh2Si2:
T*: crossover temperature for the Kondo breakdown.
T* meets TN line the QCP.
Changes from small FS to large FS crossing the T* line?
TFL: FL region.
CoRhIr:
Negative pressure, suppressing AFM.
T* line reaches zero in AFM, at QCP and away from QCP.
T* is determined by Hall effect and thermal properties.
Problem:
Impossible to study the real reconstruction of FS.
S. Friedemann et al, Nature Phys. (2011)

## Slide 6
(H. von Lohneysen,‘96)
CeCu6-xAux: local vs. SDW QCP for doping vs. field-induced QCP?
E/T scaling of the inelastic neutron-scattering cross-section S in CeCu5.9Au0.1 : =0.75.
CeCu5.8Au0.2: field induced QCP at B~0.35T! HMM scenario fits better!
A. Schröder, Nature (2000)
O. Stockert, PRL(2007)

## Slide 7
Quantum criticality: various tuning parameters
N. Harrison et al, PRL (2007)
Pressure: Small FS to large FS at Pc=2.6 GPa Delocalization of f-electrons?
Magnetic field: Polarization of f-electron moments Small FS above Hc=61T.
Issues:
Quantum criticality tuned by various parameters (e.g., H, P …)
 Similar or different?
Direct evidence of Fermi surface reconstruction around the QCP?

## Slide 8
Heavy fermions CeMIn5 (M = Co, Rh, Ir)
Co
3d7 4s2
Ni
3d8 4s2
Fe
3d6 4s2
Rh
4d8 5s1
Ir
5d7 6s2
Pd
4d10 5s0
Ru
4d7 5s1
Pt
5d10 6s0
Os
5d6 6s2
Cu
3d10 4s1
Mn
3d5 4s2
1) CeCoIn5 (M=Co) – heavy fermion SC
C/T = 290 mJ mol-1 K-2 at Tc = 2.3 K
2) CeIrIn5 (M=Ir) – heavy fermion SC
C/T = 700 mJ mol-1 K-2 at Tc = 0.4 K
3) CeRhIn5 (M=Rh) – AFM
C/T = 420 mJ mol-1 K-2 at TN = 3.7 K,
Q = (1/2, 1/2, 0.297), meff = 0.79 B (0.84)
M=Co, Rh, Ir
In(2) site
In(1) site
Petrovic et al. JPCM 13, (2001)
M-In
Ce-In
Ce-In

## Slide 9
CeRhIn5: Localized 4f-electrons?
N. Harrison et al, PRL (2004); H. Shishido et al, JPSJ (2002); D. Hall et al., PRB (2001);S. Elgazzar., PRB (2004)
Comparison of exp. and theory.
Calculations assuming localized f-el.
Similarity between LaRhIn5 and CeRhIn5

## Slide 10
T. Park et al, Nature (2006)
G. Knebel et al (2006)
G. Knebel et al (2006)
CeRhIn5: pressure induced QCP
Magnetic order disappears around 1.9 Gpa where TN=Tc.
Pressure induced QCP at pc=2.4GPa.
Field induced magnetism inside the superconducting state.

## Slide 11
Dramatic changes of Fermi surface at p-induced QCP
Dramatic changes of dHvA frequencies at Pc =2.4GPa.
Sharp enhancement of m* at Pc.
Evidence for local AFM QC or valence QC?
Complications of magnetic field effect on the AFM transition!
H.Shishido et al, JPSJ (2005)

## Slide 12
CeRhIn5: Any new physics in high field?
T=0K

## Slide 13
T. Takeuchi et al., JPSJ (2001)
S. Raymond ey al, JPCM (2007)
The magnetic order and its field dependence in CeRhIn5
k=(1/2, 1/2, 1/4)
(1/2, 1/2, 0.298)
(1/2, 1/2, 0.298)
HM~2.5T: metamagnetic transition from incommensurate AFM to commensurate one.
AFM seems to be suppressed by applying a magnetic field of 50T.
Notes: CeRhIn5 is a heavy fermion AFM with an incommensurate magnetic structure. It shows rich properties in a magnetic field. For example, there exists a metamgnetic transition around 2.2T and the magnetic transition seems to be suppressed at very high magnetic field, over 50T. An important question is whether there exists a field-induced QCP in CeRhIn5? If so, what new physics can we learn from it? In order to address this problem, we have studied the specific heat and the dHvA effect in a pulsed magnetic field and obtained some important findings.

## Slide 14
Experimental setup for ac specific heat measurements in a pulsed magnetic field
Yoshimitsu Kohama et al, Rev. Sci. Ins. (2010)

## Slide 15
Thank you!

## Slide 16
P. Gegenwart et al, Nature Physics (2008)
Magnetic quantum criticality: Two scenarios
SDW QCP
Local QCP
Parameter  can be tuned by doping, pressure and magnetic field.
E*loc characterizes the breakdown of the entangled Kondo singlet state.
Critical modes: fluctuations of magnetic order parameter (SDW type); additional modes related to the breakdown of Kondo effect (local QCP).
f electrons: itinerant (large Fermi surface) or localized (small Fermi surface)?
CeCu2Si2, CeNi2Ge2…
YbRh2Si2, CeCu1-xAux
Local QCP
P. Gegenwart et al, Nature Physics (2008)

## Slide 17
dHvA effect and Fermi surface topology
Landau quantization:
Quantization of orbital motion of a charged particle in a magnetic field.
Allowed orbits are confined in a series of Landau tubes, constant energy surfaces in k-space.
Magnetization, resistivity etc: periodic function of 1/B.
dHvA effect:
Fi: oscillatory “dHvA” frequency;
Si: Fermi surface extremal cross-section in plane perpendicular to B.
Fermi surface topology:
Conditions for the dHvA effect:
Large magnetic field and low temperature
For m* = 100 me: B/T >> 75 T/K
HF: very high fields are required
High quality samples

## Slide 18
Measurements of dHvA effect
in a pulsed magnetic field
Induced voltage :
V=d/dt
(: magnetic flux, surface integral of B through the coil)
B=0(H+M)
V  dM/dt=(dM/dH)(dH/dt)
(V=0 for empty compensated coil)
Magnetic susceptibility
 V/(dH/dt)
dH/dt measured by an additional coil surrounding the signal coil.
Coil compensation:
When the probe is used, the induced voltages from both the signal coil and the compensation coil are amplified. A fraction of the voltage from the compensation coil is then added to or subtracted from the signal coil voltage to null out any remaining induced voltage.
H
sample
signal coil
compensation
coil